

**DECOSET**

**DESCRIPTION**

Styrene Acrylic based, plasticizer, waterproofing solutions, easy to apply , long lasting, matt looking, water based, white, liquid membrane waterproofing material.

**APPLICATION AREA**

Concrete, water and moisture impermeability in buildings, plaster, brick, tile, briquette, gas concrete, corrugated and non-corrugated roofing boards, boards and terraces with vertical and horizontal surfaces on all surfaces , window sills, drips, pool, cistern, water tanks, channels etc. places usable.

**FEATURES**

* Good adhesion to the surface.
* Long life.
* Resistant to UV rays.
* Water based; odorless, does not harm human health and the environment.

**SURFACE PREPARATION**

All kinds of dirt on the application surfaces, oil, blistered paint and dust removed, surface defects should be corrected

**APPLICATION INSTRUCTIONS**

* DECOSET app is made in three layers.
* DECOSET for the first primer coat is diluted with approximately 50% water and applied to the surface.
* For the second layer, DECOSET is applied with 25% water and the third layer with 10-15% water and applied to the surface.
* The waiting time between the floors is at least 6 hours.
* During and after the application 24 hours, lowest ambient temperature +5 °C, highest +35 °C should be noted.

**DRYING TIME**

Touch time at 23 ° C for 5-6 hours, The full drying time is 24 hours.

**PACKING**

20 Kg

**THEORETICAL CONSUMPTION**

Surface smoothness, for three-coat application depending on absorbency and application techniques;

Vertical Application Consumption:

-1 lt with 1,5 – 2,0 m²,

-1 kg with 1,0 – 1,5 m2 area is coated.

- 1 m2 area for material consumption 500 – 660 ml and 660 – 1000 gr.

Horizontal Application Consumption:

-1 lt with 0,90 – 1,35 m²,

-1 kg with 0,60 – 1,00 m2 area is coated.

- 1 m2 area for material consumption 750 – 1100 ml and 1000 – 1500 gr

**STORAGE**

In unopened package, Cool and dry place, protected from direct sunlight, +5˚C with +35˚C between 1 year can be stored.

**Harmfulness Expressions**

* H 362 May cause harm to a breastfed child.
* H 412 Long lasting in aquatic environment, harmful effect.

**PRECAUTIONS**

* P 102 Keep out of reach of children.
* P 260 Do not breathe dust / fume / gas / mist / vapor / spray.
* P 263 During Pregnancy / avoid contact when giving breast milk
* P 270 Do not eat, drink or smoke when using this product
* P 301+P 310 When swallowed; Call the national poison center telephone number 114 or the doctor.
* P 501 Dispose of contents / container in accordance with local / regional / national / international regulations .
* Do not use product packaging for food storage.

*note: For more technical information, see Material Safety Data Sheet (MSDS) of the product .*