

 **TORNADO** **GOLD**

**DESCRIPTION**

Acrylic emulsion based decorative coating with silky gold mother-of-pearl finish consisting of metallic pigments

**APPLICATION** **AREA**

On all the interior walls, plaster, gross concrete and timber surfaces; it is used together with its appropriate primer after the surface preparation.

**FEATURES**

•TORNADO GOLD provides a glittering decorative view by its metallic pigments content

. •Live and bright pigments give a pleasant brightness for the surface.

•Via its high water vapor permeability; it provides the vapor to be discharged and the surface to breath. •Via its water-based property, it is harmless to human health and environment.

• It provides a pleasant odor for the application environments via its perfume property. **UYGULAMA** **TALİMATI**

**SURFACE** **PREPARATION**

•After removing all kinds of dirt, grease, bloated paint and dust from the application surface, the surface defects should be corrected by ACRYLIC PUTTY THIN and undercoated with DECOPRIMER.

**APPLICATION** **INSTRUCTIONS**

•After surface preparation, TORNADO GOLD is applied as two layers by a steel trowel according to the requested effect.

•The waiting time before applying the second layer is min. 6 hours

•The environment of application should not be kept under +5 ° C and above +35 ° C within 24 hours during and after the application.

**DRYING** **TIME**

The contact time is 5-6 hours thorough-dry time is 24 hours in environment of 23oC.

**PACKAGING**

 2,5 KG

**THEORITICAL** **CONSUMPTION**

Depending on surface smoothness, porosity and application methods, for a single coat application:

With 1 liter of paint 7,5 – 9,0 m² area, with 1 kg of paint 6,5 – 8,0 m2 area can be painted. Paint consumption for 1 m2 area is 110 - 130 ml and 125 - 150 gr.

**STORAGE**

Store in enclosed packaging for 1 year between +5oC to +35Oc

**PRECAUTIONARY** **STATEMENTS**

**P** **102** Keep out of reach of children

**P** **301+** **P** **310** IF SWALLOWED: Immediately call a POISON CENTRE or doctor/physician

*Note:* *For* *more* *technical* *information,* *please* *check* *the* *Material* *Safety* *Data* *Sheet* *(MSDS)* *of* *the* *product*